o
Electron-Phonon Coupling
in graphene
Claudio Attaccalite
Trieste 10/01/2009

---
Outline
- DFT: ground state properties
  Many-Body Perturbation Theory: excited state properties
- Quasi-Particle band structure
- Phonons and Electron-Phonon Coupling (EPC) in DFT (LDA and GGA)
- It is possible to go beyond DFT and obtain an accurate description of the EPC
- Recent Raman experiments can be reproduced completely ab-initio
[Speaker Notes: Here, we show that: i) the GW approach, which provides the most accurate ab-initio treatment of electron correlation, can be used to compute the electron-phonon interaction and the phonon dispersion; ii) in graphite and graphene, DFT (LDA and GGA) underestimates by a factor 2 the slope of the phonon dispersion of the highest optical branch at the zone-boundary and the square of its electron-phonon coupling by almost 80%; iii) GW reproduces both the experimental phonon dispersion near K, the value of the EPC and the electronic band dispersion; iv) the B3LYP hybrid functional2 reproduces well the experimental phonon dispersion, but overestimates both EPC and band dispersion; v) within Hartree-Fock the graphite structure is unstable.]

---
Density Functional Theory
The ground state energy is expressed in terms of the density and
an unknown functional Exc
E[n]=T_0[n] - {e^2} over 2 int { {n(r) n(r') }over { abs {r-r'} } dr dr'} + E_{xc}[n] - int { n(r) v_{xc}(r) dr}
Kohn-Sham eigenfunctions are obtained from
left ( - {hbar^2 } over {2m } {partial^2} over {partial r^2} + V_{SCF}(r) right ) %PSI_n(r) = %epsilon_n %PSI_n(r)
Usually Exc in the local density approximation (LDA) or the general gradient approximation (GGA) successfully describes the ground state properties of solids.

---
Beyond DFT:
Many-Body Perturbation Theory
Starting from the LDA Hamiltonian we construct the
Quasi-Particle Dyson equation:
[T+V_h + V_{ext}] %PSI_{n,k}(r) + int { dr' %SIGMA (r,r';E_{n,k}) %PSI_{n,k}(r')} = E_{n,k} %PSI_{n,k}(r)
: Self-Energy Operator;
: Quasi-particle energies;
%SIGMA
E_{n,k}
... following Hedin(1965): the self-energy operator
is written as a perturbation series
of the screened Coulomb interaction
%SIGMA = i G W + dotsaxis
W = %epsilon^{-1} v
G: dressed Green Function
W: in the screened interaction

---
Quasi-Particles Band Structure
In GW the bandwidth is increased and consequently the Fermi velocity vF is enhanced
Comparison of GW with ARPES experiments
for graphite A. Gruenis, C.Attaccalite et al. PRL 100, 189701 (2008)

---
what about the phonons?

---
Motivations
   Electron-Phonon Coupling (EPC)
determines:
- Kohn anomalies
- Phonon-mediated superconductivity
- Jahn-Teller distortions
- Electrical resistivity
[Speaker Notes: The electron-phonon coupling (EPC) is one of the fundamental quantities in condensed matter. It determines phonon-dispersions and Kohn anomalies, phonon-mediated superconductivity, electrical resistivity, Jahn-Teller distortions etc. Nowadays, density functional theory within local and semi-local approximations (DFT) is considered the ”standard model” to compute ab-initio the electron-phonon interaction and phonon dispersions. Thus, a failure of DFT would have major consequences in a broad context. In GGA and LDA approximations,]

---
Phonon dispersion of Graphite
(IXS measurements) and DFT calculations
M. Mohr et al. Phys. Rev. B 76, 035439 (2007)
J. Maultzusch et al. Phys. Rev. Lett. 92, 075501 (2004)
L. Wirtz and A. Rubio, Solid State Communications 131, 141 (2004)
[Speaker Notes: Phonon dispersion of graphite. Lines are DFT calculations, dots and triangles are IXS measure-ments from Refs. 8,9, respectively.]

---
Phonon dispersion close to K
In spite of the general good agreement the situation is not clear close to K

---
Phonon dispersion close to K
In spite of the general good agreement the situation is not clear close to K

---
Raman Spectroscopy of graphene
[Speaker Notes: Time: 0.00 to 0.75 (min)‏ Whenever a new material is found, Raman spectroscopy is among the first steps in order to characterize it. Graphite itself is an old and intensively studied material. However its building-block, a single-layer of graphene has only recently been transfered to a substrate Due to the high structural anisotropy – it is composed of stacked layers which are only weakly coupled - few-layer graphene is a promising playground to investigate the crossover from 3D to 2D physics. Raman spectrocopy is an appropiated tool, since it probes vibrational properties and beside of that also the electronic bandstructure via the mechanism of double-resonant Raman scattering.]

---
Raman G-line
Single-resonant
G-line
K
k
at  point, k~0
→ G-line
phonon

---
Raman D-line
{
dispersive
K
K'
%tendto %omega_q
{
q

---
.... but also from Raman....

---
 How to calculate phonons in GW?
D^{%alpha %beta}_{st} (q) = {partial^2 E} over {partial u_s^{%perthousand %alpha} (q) partial_t^{ %beta}(q) }
Phonon frequencies (squared) are
eigenvalues of the dynamical matrix
Ideal solution: calculate total energy and its derivatives in GW
Problem: how to calculate total energy in GW
(questions of self-consistence and of numerical feasibility)‏
[Speaker Notes: Time: 1.50 to 2.50 (min)‏ Before showing results on few-layer graphene let me shortly remind you of Raman spectrosopy on graphite. A typical Raman spectrum is shown at the bottom of the slide with peaks corresponding to phonons created in the exposed graphite. Such an inelastic process is schematically depicted above: we see the electronic bandstructure with two bands crossing at the K point. We choose the one of graphene for simplicity. First, an electron is resonantly excited from the valence to the conduction band by an incoming photon. In a next step a phonon with vanishing wave vector is created, the electron will relax to a virtual state from where it will recombine, emitting a photon with a lower energy: it is this energy difference which is plotted in the horizontal axis. This so-called single-resonant process will give rise to the G line at 1582 /cm, and with a two-phonon emitted we get its overtone, the G‘ line.]

---
Electron-Phonon Coupling
and dynamical matrix
%omega_q = sqrt { D_q /m }
D_q = B_q + P_q
P_q = {4} over {N_k} sum from{k} { { {abs{D_{(k+q) %pi^{%perthousand},k %pi }}}^{2} } over {%epsilon_{k,%pi}-%epsilon_{k+q,%pi^{%perthousand}}} }
-bands self-energy
D_{(k+q) %pi^{%perthousand},k %pi } = langle k+q,%pi^{%perthousand} abs{%DELTA V} k,%pi rangle
Electron-Phonon Coupling

---
Phonon dispersion without dynamical matrix of the p bands
tilde %omega = sqrt { B_q/m}

---
..but using GW band structure provides a worse result
%omega_q = sqrt { (B_q + P_q) /m }
because
P_q = {4} over {N_k} sum from{k} { { {abs{D_{(k+q) %pi^{%perthousand},k %pi }}}^{2} } over {%epsilon_{k,%pi}-%epsilon_{k+q,%pi^{%perthousand}}} }
where
In fact the GW correction to the electronic bands alone results in a larger denominator providing a smaller phonon slope and a worse agreement with experiments.

---
Frozen Phonons Calculation of the EPC
The electronic Hamiltonian for
the  and * bands
can be written as 2x2 matrix:
H(k,0) = left ( binom{hbar v_f k}{0} binom{0}{-hbar v_f k} right )
a distortion of the lattice according to the G-E2G
H(k,u) = H(k,0) + {partial H(k,0) } over {partial u } u + O(u^2)
{partial H(k,0) } over {partial u } = 2 sqrt { langle D_{%GAMMA}^2 rangle_F } left ( binom{a}{b^%perthousand} binom{b}{-a} right )
where:
langle D_{%GAMMA}^2 rangle_F = lim _{d rightarrow 0 } { { 1 } over { 16 } left ( { %DELTA E_%GAMMA} over { d} right )^2 }
!!!!!
If we diagonalize H(k,u) at the K-point
We can get the EPC for the p bands with a frozen phonon calculation!!!

---
EPC and a in different approximations
To study the changes on the phonon slope we recall that Pq is
the ratio of the square EPC and band energies
P_q = {4} over {N_k} sum from{k} { { {abs{D_{(k+q) %pi^{%perthousand},k %pi }}}^{2} } over {%epsilon_{k,%pi}-%epsilon_{k+q,%pi^{%perthousand}}} }
Thus we studied:
%alpha_q = langle D^2_q rangle_F / %DELTA %epsilon_g
Hartree-Fock equilibrium structure

---
...the same result ...
but with another approach
Dirac massless fermions
+
 Renormalization Group
D. M. Basko et I. L. Aleiner
Phys. Rev. B 77, 0414099(R) 2008
Electron and phonon
renormalization
 of the EPC vertex

---
How to model the phonon dispersion
to determine the GW phonon dispersion we assume
r^{GW}={%alpha^{GW}_K} over { %alpha_K^{DFT}} simeq {P^{GW}_K} over { P_K^{DFT}}
where
%omega_q^{GW} simeq sqrt { (B_q^{GW} + r^{GW} P_q^{DFT})/m}
We assume Bq constant because it is expected
to have a small dependence from q and fit it from
the experimental measures
B^{GW}_q simeq B_K^{GW}
The resulting K A′ phonon frequency is 1192 cm−1 which is our best estimation and is almost 100 cm−1 smaller than in DFT.

---
Results: phonons around K
Phys. Rev. B 78, 081406(R) (2008) M. Lazzeri, C. Attaccalite, L. Wirtz and F. Mauri

---
Results: the Raman D-line dispersion

---
Conclusions
- The GW approach can be used to calculate EPC
- In graphene and graphite DFT(LDA and GGA) underestimates the phonon dispersion of the highest optical branch at the zone-boundaries
- B3LYP gives a results similar to GW but overestimates the EPC
- It is possible to reproduce completely ab-initio the Raman D-line shift

---
Acknowledgment
1) The support from:
2) My collaborators
M. Lazzeri, L. Wirtz, A. Rubio and F. Mauri
Codes I used:
http://www.yambo-code.org
http://www.pwscf.org
http://www.crystal.unito.it

---
The case of Doped Graphene
With doping graphene evolves from a semi-metal to a real metal.
Therefore the effective interaction felt by the electrons starts to be weaker due
the stronger screening of the Coulomb potential.
Solid State Commun. 143, 58 (2007) M. Polini et al.
http://arxiv.org/abs/0808.0786 C. Attaccalite et al.

---
Electron-phonon Coupling at K
LDA results is recovered in doping graphene
WORK IN PROGRESS . . .

---
Tuning the B3LYP
The B3LYP hybrid-functional has the from:
E_{xc} = (1-A) dot (E_x^{LDA} + B dot E_x^{BECKE}) + A dot E_x^{HF} + (1-C) dot E_c^{VWN}+C dot E_c^{LYP}
B3LYP consist of a mixture of Vosko-Wilk-Nusair and LYP correlation part Ec
and a mixture of LDA/Becke exchange with Hartree-Fock exchange
The parameter A controls the admixture
of HF exchange in the standard B3LYP is 20%
It is possible to reproduce GW results
tuning the non-local exchange in B3LYP !!!!!

---
Many-Body perturbation Theory 2
Approximations for G and W (Hybertsen and Louie, 1986):
• Random phase approximation (RPA) for the dielectric function.
• General plasmon-pole model for dynamical screening.
we use the LDA results as starting point
G approx G^{LDA}
and so the Dyson equation becomes
(T + V_h + V_{ext} + V_{xc} ) %PSI_{n,k} int { %SIGMA'(r,r'; E_{n,k}) %PSI_{n,k} } = E_{n,k} %PSI_{n,k}(r)
%SIGMA'(r,r'; E_{n,k}) = %SIGMA'(r,r'; E_{n,k}) -%delta(r,r') V_{xc}(r)

---
 Raman spectroscopy of graphene
Single-resonant
G-line
D-line
phonon
K
k
at  point, k~0
→ G-line
dispersive
TO mode between K and M
graphite
2.33 eV
G
D‘
G‘
D
Ref.: S. Reich, C. Thomsen, J. Maultzsch, Carbon Nanotubes, Wiley-VCH (2004)‏
[Speaker Notes: Time: 1.50 to 2.50 (min)‏ Before showing results on few-layer graphene let me shortly remind you of Raman spectrosopy on graphite. A typical Raman spectrum is shown at the bottom of the slide with peaks corresponding to phonons created in the exposed graphite. Such an inelastic process is schematically depicted above: we see the electronic bandstructure with two bands crossing at the K point. We choose the one of graphene for simplicity. First, an electron is resonantly excited from the valence to the conduction band by an incoming photon. In a next step a phonon with vanishing wave vector is created, the electron will relax to a virtual state from where it will recombine, emitting a photon with a lower energy: it is this energy difference which is plotted in the horizontal axis. This so-called single-resonant process will give rise to the G line at 1582 /cm, and with a two-phonon emitted we get its overtone, the G‘ line.]

---
Electron-Hole Coupling