Luminescence of
hexagonal boron nitride monolayer
Claudio Attaccalite
P. Lechifflart, F. Paleari,
D. Sangalli
Advanced Quantum Materials (2023)

---
Hexagonal Boron Nitride
h-BN is a layered
crystal homo-structural to graphite.
As graphite, h-BN can be easily exfoliated, and for this reason it finds applications as lubricant .

---
Use of hBN in condensed matter
Single photon emitters
Encapsulated 2D materials

---
Hexagonal Boron Nitride
h-BN has a large band gap and it’s transparent
h-BN emits light in the ultraviolet

---
UV light emitters

---
Band structure of hBN

---
Internal quantum yield
Diamond
ZnO
Bright Luminescence from Indirect and Strongly Bound Excitons in h-BN
L. Schué, L. Sponza et al.,
Phys. Rev. Lett. 122, 067401(2019)
0.1%
50%

---
Internal quantum yield
Diamond
hBN
ZnO
Bright Luminescence from Indirect and Strongly Bound Excitons in h-BN
L. Schué, L. Sponza et al.,
Phys. Rev. Lett. 122, 067401(2019)
45%
0.1%
50%

---
Strong bound
excitons in h-BN
Ellipsometry Study of Hexagonal Boron Nitride Using Synchrotron Radiation: Transparency Window in the Far‐UVC
Luis Artús, et al. Advanced Photonics Research 2 (5), 2000101 (2021)
No-exciton spectrum

---
Exciton-phonon coupling
The strong exciton confinement enhances the coupling with phonons
Theory of phonon-assisted luminescence in solids:
application to hexagonal boron nitride
E. Cannuccia,et al. Phys. Rev. B 99, 081109(R) (2019)

---
Monolayer hexagonal BN
First Luminescence measurement on epitaxial grown monolayer boron nitride on graphite substrates
Nature Communications volume 10, Article number: 2639 (2019)

---
From bulk to monolayer…..
Direct observation of the band structure in bulk hexagonal boron nitride
H. Henck, et al.
PRB 95, 085410(2017)

---
Luminescence spectra
Nature Communications volume 10, Article number: 2639 (2019)

---
Luminescence spectra … again
Monolayer Boron Nitride: Hyperspectral Imaging in the Deep Ultraviolet
A. Rousseau et al.
Nano Lett. 2021, 21, 23, 10133–10138

---
Luminescence spectra … again
Monolayer Boron Nitride: Hyperspectral Imaging in the Deep Ultraviolet
A. Rousseau et al.
Nano Lett. 2021, 21, 23, 10133–10138
“Scalable Synthesis of Monolayer Hexagonal Boron Nitride on Graphene with Giant Bandgap Renormalization."
Wang et al. Advanced Materials 34.21 (2022).

---
A new theoretical approach

---
Validation

---
Theory vs experiments

---
Conclusion
- Strong phonon assisted luminescence of bulk BN is due to the exiciton localization
- Monolayer-BN presents only direct light-emission, the phonon assisted one is too weak
- We developed a new approach to study phonon-assisted transitions
Theory of phonon-assisted luminescence in solids: application to hexagonal boron nitride
E. Cannuccia,et al. Phys. Rev. B 99, 081109(R) (2019)
Ellipsometry Study of Hexagonal Boron Nitride Using Synchrotron Radiation: Transparency Window in the Far‐UVC, Luis Artús, et al. Advanced Photonics Research 2 (5), 2000101 (2021)
First-principles study of luminescence in hexagonal boron nitride single layer: Exciton-phonon coupling and the role of substrate
P. Lechifflart, et al. Phys. Rev. Mat. 7, 024006 (2023)

---
Direct or
indirect excitons

---
The role of substrate